## Slide 2
Fotomoltiplicatore
una finestra nell’involucro di vetro
entrata dei fotoni
ottica elettronica
elettrodi che accelerano e focalizzano i fotoelettroni.
Fotocatodo:
Converte I fotoni incidenti in fotoelettroni.
Moltiplicatotre di elettroni
Elettrodi che moltiplicano la carica mediante l’emissione di elettroni secondari. (106-107)
Anodo
Raccoglie gli elettroni prodotti dall’ultimo dinodo.

## Slide 3
Un fotomoltiplicatore è costituito da:
-Un fotocatodo.
-Un sistema di focalizzazione e accelerazione (gestito dal sistema elettroottico d’ingresso).
-Uno stadio moltiplicatore di corrente costituito da elettrodi (dinodi) che utilizza il fenomeno dell’emissione secondaria di elettroni.
-Un anodo.

## Slide 4
a free electron cannot absorb the photon and conserv momentum
    Effect always on bound electrons with nucleus absorbing recoil momentum
Photoelectric Effect
Photoelectric effect on potassium (used in photocathodes)
limite bassa frequenza (alta l) per produzione di fotoelettroni

## Slide 5: Photoelectric Absorption
Photon deposits its total energy in a single interaction with an absorber atom.
A photoelectron is emitted with the energy
where Eb is the binding energy of the photoelectron.
Photoelectric absorption dominates at rather low energies, but the cross section increases rapidly with Z.
n = 4 - 5
Low energy: Eg < 100 KeV
Soglia per effetto fotoelettrico:
Eg = hn = Ee + Eb;
hnmin = Eb ~ 2-10 eV
Frequenza di soglia
Numero di e emessi  intensità della radiazione
Energia cinetica e emessi  frequenza della radiazione

## Slide 6
E(eV) = 1240/λ ( nm)

## Slide 7
Window materials
Because ultraviolet radiation tends to be absorbed by the window material, the short wavelength limit is determined by the ultraviolet transmittance of the window material.
MgF2 crystal
A magnesium fluoride (MgF2) crystal is used as a practical window material because it offers very low transmission of vacuum ultraviolet radiation down to 115 nanometers.
Sapphire
Sapphire glass has a short wavelength cutoff in the neighborhood of 150 nanometers, which is slightly shorter than that of synthetic silica.
Synthetic silica
Synthetic silica transmits ultraviolet radiation down to 160 nanometers and in comparison to fused silica, offers lower levels of absorption in the ultraviolet region.
UV glass (UV-transmitting glass)
The short wavelength cutoff of the UV glass extends to 185 nanometers.
-------------------------------
Borosilicate glass
This is the most commonly used window material. The borosilicate glass does not transmit ultraviolet radiation shorter than 300 nanometers. It is not suited for ultraviolet detection shorter than this wavelength.

## Slide 9
Spectral transmittance of window materials

## Slide 10
SIDE-ON
C
A
HEAD-ON
A
C
Il fotocatodo
Il fotocatodo converte la luce incidente in corrente di elettroni sfruttando l’effetto fotoelettrico. Esso è costituito da una sostanza fotoemittente depositata in un sottilissimo strato sulla parete interna della finestra di ingresso del fotomoltiplicatore. L'efficienza di conversione fotoelettrica varia fortemente con la frequenza della luce incidente e con la struttura del materiale.

## Slide 11
Il fotocatodo
Processo a 3 fasi:
  foto-ionizzazione della molecola
  propagazione degli elettroni nel catodo
  fuga degli elettroni nel vuoto
Reflective a) and semitransparent b) PCs
SIDE-ON
HEAD-ON

## Slide 12
Photocatode type

## Slide 13
Fotocatodo
Gli elettroni vengono emessi con energia cinetica:
La maggior parte degli elettroni prodotti diffondono nel fotocatodo rilasciando parte della loro energia e solo quelli che raggiungono l’interfaccia tra il fotocatodo e il vuoto con energia sufficiente a superare il potenziale di estrazione (Ф~1eV) riescono ad uscire e vengono quindi accelerati e focalizzati da un elettrodo sul primo dinodo.
Efficienza quantica
Sottile film di materiale fotoemissivo posto su una finestra in vetro otticamente trasparente che costituisce l’ingresso del fototubo. I fotoelettroni sono emessi dalla parte opposta rispetto a quella da cui proviene la luce incidente.
La fotoemissione è un processo probabilistico.
L’efficienza di conversione dei fotoni luminosi in fotoelettroni varia fortemente in
relazione alla frequenza della luce incidente e alla struttura del materiale
Φp(ν,x)=Φp(ν,0) x [1-r(ν)] x exp α(ν)x
Fotoni che entrano nel fotocatodo
1/α = lunghezza di penetrazione,
distanza 63% fotoni assorbiti

## Slide 14
Fotocatodo
Materiali usati per il fotocatodo:
Gli elettroni atomici sono liberi di muoversi nel materiale. Un fotoelettrone generato ad una profondità x perde molta energia nel muoversi verso la superficie a causa degli urti con questi elettroni liberi. Anche alta reflettivita’ ottica.
La probabilità di raggiungere la superficie con energia sufficiente per superare la barriera di potenziale è bassa. In metalli 2 eV.
Si usano materiali di piccolo spessore escape depth 1nm. (10-50 °A) UV (100°A)
La struttura a bande separata da una gap fa sì che solo pochi elettroni (quelli nella banda di conduzione) sono liberi (dipende dalla temperatura). Gli urti con gli elettroni liberi sono ridotti.Possono avvenire urti con gli elettroni legati ma si ha poca energia trasferita (la massa degli atomi).bassa reflettivita’
efficienza quantica ~ 0.1%
efficienza quantica ~ 10-30%
La probabilità di raggiungere la superficie è alta.
Escape depth ed efficienza di conversione sono più alte. (qualche centinaio di nm a decine di nm)
La maggiore parte dei fotocatodi è fatta di materiale semiconduttore (antimonio Sb) più metalli alcalini.
Metalli:
Semiconduttori:
1 Å= 0,1 nm = 10−4 μm

## Slide 15
Absorption coefficients α as functions of photon energy hν for various photoemissive layers
Φp(ν,x)=Φp(ν,0) x [1-r(ν)] x exp α(ν)x
exp α(ν)x
1/α = lunghezza di penetrazione,
distanza 63% fotoni assorbiti

## Slide 16
Work functions F of pure metals
F
For most metals F is greater than 3 eV. Only in the alkali metals (Li, Na, K, Rb, Cs) is it low enough for photoemission to occur in response to visible light.

## Slide 17
The most used photocathode materials are silver-oxygen-caesium (AgOCs), antimony-caesium (SbCs), and the bi and trialkali compounds SbKCs, SbRbCs, and SbNa2KCs. They are limited at long wavelengths by the photoemission threshold of the material, and at short wavelengths by the transmission of the window. Table 1.1 gives the characteristics of some standard photocathodes.
The sensitivity curves of bi and trialkali cathodes can be shifted toward the long wavelengths at the expense of blue sensitivity, by increasing their thickness; the trialkali S2ORb photocathode (sometimes called S25) is an example.
Semiconductors with negative electron affinity such as GaAs, GaInAs, and GaInAsP, have sensitivities extending into the near-infrared

## Slide 18
Composti metalli alcalini (elettrone poco legato) e semiconduttori

## Slide 19
Energia di Fermi e lavoro di estrazione (funzione di lavoro)
lavoro di estrazione o funzione lavoro è l'energia minima che occorre fornire per estrarre un elettrone da un metallo. Questa energia dipende dal tipo di metallo e si aggira in genere intorno a qualche elettronvolt. All'interno di un materiale gli elettroni di conduzione al massimo possiedono un'energia pari al livello di Fermi a temperatura T=0 K, ovviamente tale energia è insufficiente a consentire agli elettroni di lasciare il materiale scavalcando la barriera energetica superficiale.
Energia di foto
emissione
Epe=F=E0-EF=hn0
lavoro di estrazione nei metalli
The photoemission threshold for pure metals is between 2 eV and 6 eV.
1.6 - 3.25 eV
=380 nm and 780 nm

## Slide 20
Simplified energy-bands diagram for a metal a) and a semiconductor b) both having the same photoemission threshold hn0. An incident photon of energy hn excites an electron at a distance x1 or x2 >x1 from the surface. In the semiconductor, the energy losses for excited electrons as they move to the surface are rather small. The electrons excited at distances x1 and x2 both have sufficient energy to escape into vacuum. In the metal, the exited electrons rapidly lose their kinetic energy in electron-electron collisions. Thus only electrons excited in the vicinity of the surface could escape into vacuum. Here EF is the Fermi level, E0 is the energy of vacuum potential barrier, EG is the bandgap of the semiconductor and EA is its electron affinity.
photons in x1
escape
photons in x1
and x2 escape
(10-50 °A)
UV (100°A)
(1000-10000 °A)
scatters preferably
on phonons
1°A=10-10 m
F=E0-EF
F=EG+EA
hn0>F
Metal
Semiconductor

## Slide 21
Energy Gap
nei semiconduttori

## Slide 22
ENERGIA di FERMI
Metallo alcalino:favorito per bassa funzione di lavoro ma interazione con altri elettroni
Semiconduttore: favorito per bassa interazione con elettroni, gap, si puo’ abbassare la
funzione di lavoro

## Slide 23: Diagramma a bande: metallo
A T = 0, tutti i livelli nella banda di conduzione sotto l’energia di Fermi EF sono riempiti con elettroni, mentre tutti i livelli al di sopra di EF sono vuoti.
Gli elettroni sono liberi di muoversi negli stati vuoti della banda anche con solo un debole campo E, → elevata conducibilità elettrica!
A T > 0, gli elettroni hanno una certa probabilità non nulla di essere termicamente eccitati da sotto a sopra il livello di Fermi.
T > 0
Funzione di Fermi
Bande di energia da riempire
EF
EC,V
Banda di conduzione
parzialmente piena
E = 0

## Slide 24: Diagramma a bande: isolante
At T = 0, la banda di valenza è piena di elettroni mentre la banda di conduzione è vuota, → conducibilità zero.
  Energia di Fermi EF è a metà di un largo gap energetico (2-10 eV) tra la banda di valenza e di conduzione.
A T > 0, gli elettroni NON sono eccitati termicamente dalla banda di valenza alla banda di conduzione →conducibilità zero.
Nota: KT a T=300K è pari a 0.0259eV, quindi <<Egap
EF
EC
EV
Banda di conduzione
(Vuota)
Banda di valenza
(Piena)
Egap
T > 0

## Slide 25: Diagramma a bande: semiconduttore non drogato
A T = 0, la banda di valenza è piena di elettroni e la banda di conduzione vuota →conducibilità zero.
  L’energia di Fermi EF è a metà di un gap piccolo (<1 eV) tra la banda di conduzione e la banda di valenza.
A T > 0, gli elettroni vengono eccitati termicamente dalla banda di valenza alla banda di conduzione, →conducibilità misurabile.
EF
EC
EV
Banda di conduzione
(parzialmente piena)
Banda di valenza
(parzialmente vuota)
T > 0

## Slide 26
electron affnity E, represents the distance between conduction band bottom and vacuum level.
Electron affinity
EG
For photocatodes sensitive to visible light, this sum EG + EEA must therefore be less than 3.25 eV (less than 1.6 eV to cover the whole visible region up to 780 nm). This condition is fulfilled in some complex semiconductors.
photoemission energy=EG+EEA
thermoionic work function=F
(T=0)
F
Semiconductors generally have work functions of 5 − 6 eV, and so can be sensitive only to wavelengths less than about 300 nm. Possible improvements!!
Nei semiconduttori

## Slide 27
Intrinseco “i”
drogaggio “p”
drogaggio “n”
Elettroni di drogaggio vanno ad aggiungersi agli elettroni collettivi, spostando il baricentro della distribuzione elettronica(livello di Fermi), per cui la funzione di Fermi viene traslata ad energie più alte.
Un drogaggio di tipo 'p’ l'introduzione di lacune impoveriscono di elettroni la distribuzione di Fermi, lasciandone inalterata la forma ma traslandone la relativa funzione verso energie più basse

## Slide 28
Energy band diagrams in the near surface region for n-doped (n), intrinsic (i) and p-doped (p) semiconductors
Fotocatodi con semiconduttore drogato p
= 5-6 eV
300 nm

## Slide 29
Semiconductor energy-band model showing negative electron affinity
P-doped semiconductor improved depositing a molecular layer of, the so called electro-positive material layer of polarized or ionized atoms with its positive pole directed towards vacuum, acts as a surface dipole. Electro-positive materials are Ba-O, Cs-F, Cs, Cs-O.
Without NEA, a photoelectron excited to conduction band travels loosing its energy in phonon-scattering, once its energy is reduced below the vacuum level it cannot escape. It travels rather short distance (typically about 100° 200 ̊A) until it recombines with a hole. The photoelectron escape depth is greatly increased in NEA

## Slide 30
Spectral Responsitivity (Sk)
Quantum efficiency (Q.E.) ρ

## Slide 31
Three main types of alkali-antimonide PCs depending on their spectral characteristics: blue-sensitive (Cs3Sb, K2CsSb, Na2KSb), green-enhanced (Rb2CsSb) and red-enhanced ((Cs)Na2KSb). They exhibit typical QE values of 20-30% at maximum, located in the blue or green spectral regions.

## Slide 32
The spectral response on long wavelengths is determined by the photocathode material and on short wavelengths by the window material.
Typical Spectral Response of Bialkali Photocathode
The window material determines the spectral response short wavelength cutoff.

## Slide 33
La composizione chimica del fotocatodo determina la risposta spettrale
Un fotocatodo ha al massimo un’efficienza quantistica del 30%

## Slide 35
Photocathode materials
Most photocathodes are made of compound semiconductors which consist of alkali metals with a low work function.
Cs-I
Cs-I is not sensitive to solar radiation and therefore often called "solar blind". Its sensitivity sharply falls off at wavelengths longer than 200 nanometers and it is exclusively used for vacuum ultraviolet detection. As a window material, MgF2 crystals or synthetic silica are used because of high ultraviolet transmittance.
Cs-Te
Cs-Te is not sensitive to wavelengths longer than 300 nanometers and is also called "solar blind" just as with Cs-I. Synthetic silica or MgF2 is usually used for the input window.
Sb-Cs
This photocathode has sensitivity in the ultraviolet to visible range. Because the resistance of the Sb-Cs photocathode is lower than that of the bialkali photocathode described later on, it is suited for applications where light intensity to be measured is relatively high so that a large current can flow in the cathode.
Bialkali (Sb-Rb-Cs, Sb-K-Cs)
Since two kinds of alkali metals are employed, these photocathodes are called "bialkali". The transmission type of these photocathodes has a spectral response range similar to the Sb-Cs photocathode, but has higher sensitivity and lower dark current. As a result, they offer enhanced sensitivity on the long wavelength side, achieving a spectral response from the ultraviolet region to around 700 nanometers.

## Slide 36
High temperature, low noise bialkali (Sb-Na-K)
As with bialkali photocathodes, two kinds of alkali metals are used in this photocathode type. The spectral response range is almost identical to that of bialkali photocathodes, but the sensitivity is somewhat lower. This photocathode can withstand operating temperatures up to 175°C while other normal photocathodes are guaranteed to no higher than 50°C. When used at room temperatures, this photocathode exhibits very low dark current, which makes it very useful in low level light measurement such as photon counting applications where low noise is a prerequisite.
Multialkali (Sb-Na-K-Cs)
This photocathode uses three or more kinds of alkali metals. High sensitivity over a wide spectral response range from the ultraviolet through near infrared region around 850 nanometers.
Ag-O-Cs
Transmission type photocathodes using this material are sensitive from the visible through near infrared region, from 400 to 1200 nanometers. Compared to other photocathodes, this photocathode has lower sensitivity in the visible region, but it also provides sensitivity at longer wavelengths in the near infrared region.
GaAsP (Cs)
A GaAsP crystal activated with cesium is used as a transmission type photocathode. This photocathode does not have sensitivity in the ultraviolet region but has a very high quantum efficiency in the visible region.

## Slide 37
GaAs (Cs)
A GaAs crystal activated with cesium is used for both reflection type and transmission type photocathodes. The reflection type GaAs(Cs) photocathode has sensitivity across a wide range from the ultraviolet through near infrared region around 900 nanometers. It demonstrates a nearly flat, high-sensitivity spectral response curve from 300 and 850 nanometers. The transmission type has a narrower spectral response range because shorter wavelengths are absorbed.
InGaAs (Cs)
This photocathode provides a spectral response extending further into the infrared region than the GaAs photocathode. Additionally, it offers a superior signal-to-noise ratio in the neighborhood of 900 to 1000 nanometers in comparison with the Ag-O-Cs photocathode. InP/InGaAsP(Cs), InP/InGaAs(Cs)
These are field-assisted photocathodes utilizing a PN junction formed by growing InP/InGaAsP or InP/ InGaAs on an InP substrate. Applying a bias voltage to this photocathode lowers the conduction band barrier, and allows for higher sensitivity at long wavelengths extending to 1.4 μm or even 1.7 μm which have up till now been impossible to detect with a photomultiplier tube. Since these photocathodes produce large amounts of dark current when used at room temperatures, they must be cooled to between -60°C to -80°C during operation.

## Slide 39
SEMITRANSPARENT PHOTOCATHODE SPECTRAL RESPONSE CHARACTERISTICS

## Slide 40
SEMITRANSPARENT PHOTOCATHODE SPECTRAL RESPONSE CHARACTERISTICS